## Slide 1
Lightweight aggregates:
Aggregate Classify according to bulk density to: ordinary, light, and heavy aggregate.
Density of lightweight aggregate <1 – 1.6gm/cm3 while ordinary aggregate is 1.8 – 2.7gm/cm3.
Characteristic properties of lightweight aggregates:
1- Thermal and sound insulation
2- Resist fire
3- Lightweight & high porosity and easy to move, transport and cut
4- Need less iron for reinforcement (lightweight concrete)

## Slide 2
Uses of Lightweight aggregates:
1- Lightweight concrete & light blocks
2- As filler in roofs and walls of Cooling stores
3- Building suspension bridges & multistory buildings
4- Water treatment as Water purification filters

## Slide 3
Classification of Lightweight Aggregates:
1- Natural Lightweight Aggregate: Diatomite, pumice, scoria & tuff, volcanic cinders, all are of volcanic origin except diatomite.
2- By-product Lightweight Aggregate: Foamed slag & fly ash, waste product from coal mines and slate quarries.
3- Manufactured Lightweight Aggregate: Firing clays, slate and shale → bloating and expansion, then rapid cooling.
Lightweight Aggregates for structural concrete in Iraq are tested according to IQS no. 2550 / 1986.

## Slide 4
Building stones:
During history use of local stones:
Pyramids 2800 years B.C built from limestone blocks, Defense and religious buildings, Winged Bull in Nineveh, Nineveh walls 5000 years B.C, Trade in ornamental stones, Facing with a veneer of natural stone 2 inches (Granite, Marble, Sandstone, Limestone and Slate).
Building stone comprises solid igneous, sedimentary, and metamorphic rocks, usable in its natural state or prepared by hand or mechanically. Building stone is a raw materials for the production of crushed aggregate and dimension stone (paving stone and construction products). Stone for several purposes is quarried from one deposit by blasting, breaking and dressing their size, shape and surface texture.

## Slide 5
Types of building stones:
Common building stones: granite, syanite, basalt, slate, gneiss, sandstone, limestone, marble, quartzite, chalk, gypsum --- etc.
IQS no.1387/1989 classify the Natural building stones in Iraq to:
1- Marble which classes to (calcite, dolomite, or travertine)
2- Sandstone which classes to (sandstone SiO2 > 60%, quartz sandstone SiO2 > 90%, quartzite SiO2 > 95%)
3- Limestone which classes to (low density, moderate density, high density)
4- Granite
The required tests according this specification are absorption, density, compressive strength, resistance to abrasion, and soundness.
Igneous rocks, quartzite, & some sandstone have high values and low place value.

## Slide 6
Features of building stone (Geological, physiomechanical & texture properties):
1- Strength, porosity and water absorption:
Should be strong, resistance to compressive strength, low porosity and water absorption.
Compressive strength α 1 / porosity α 1 / water absorption
Compressive strength influenced by, degree of crystallization, grains size, pores size, rock texture, type of cement in sedimentary rocks, and direction of bedding. Fine grains (granite), interlocking massive texture (quartzite), and well cemented with siliceous cement (sandstone) are stronger, but Porous stones (sandstone, chalk, and shale) are weak.

## Slide 7
2- Durability of stone:
Should be Compact, homogeneous, and nonabsorbent.
Durable stone means long lasting under temperature variation (day & night, or summer & winter), surface expands more than inner part (differential stresses).
Durability of stones are tested as soundness test (Freezing and thawing), immersion the stone 18h in a saturated solution of Na2SO4 or MgSO4.
Cleopatra needle persisted 3000 years in Egypt but start decaying after 25 years in New York (spallation and exfoliation) as a result of climatic change and industrial pollution.

## Slide 8
3- Stone decay causes of stone damage:
Physical (frost action of water), and chemical (acid rain). An increases in CO2 and SO2 levels in the atmosphere as a result of industrial processes (H2CO3 , H2SO4 emission) have serious effects especially on limestone buildings. So stones must be resistant to climatic effects.

## Slide 9
4- Pores size distribution:
Movement of water by capillarity through pores, in small pores (fine) water rise rapidly in comparison with large ones.
5- Spacing of joints & bed thickness:
Stone beds must be free from closely spaced joints, so easy to cut stone blocks.
6- Appearance after polish: Polishing depend on stone hardness.
7- Colour: Colour vary about mineral content variation.

## Slide 10
Economic features in consideration:
1- Easy of quarrying and processing
2- Thickness of overburden rocks and stone beds
3- Distance to the quarry and roads state
4- Drainage of quarry
5- Processing: used as quarried, after cutting into sizes, after dressing by calcination, crushing, sieving, and washing.