## Slide 1
Building and Construction materials:
It is any materials which is used for construction purposes. Many naturally occurring substances such as clay, rock, & sand, many industrial substances such as cement, plaster, & glass.
It comprise a great group of non-metallic materials for social and industrial developments (building schools, hospitals, health centers, road pavement, residential complexes, dams, and airports ---etc.) need finding and locating raw material resources such as those listed in the following table:

## Slide 2
Product | Sources | Desirable properties
Dimension stone and | limestone, hard sandstone, | regular widely spaced bedding
Ornamental stone | granite, marble, | & joints, high compressive
 | travertine, gypsum | strength, resistance to
 |  | weathering especially in
 |  | industrial regions
Roofing stone (Slate) | strongly cleaved fine | Regular closely spaced
 | grained metamorphic | cleavage, resistance to
 | rocks (Slate) | weathering

## Slide 3
Road stone | crushed basalt, fine granite | Resistance to abrasion, fine-
 | , quartzite, flint, industrial | medium grain size, low
 | waste, in combination | porosity, binds well with
 | with bitumen | bitumen
Aggregate: for concrete |  | 
(cement + sand + gravel), | sand and gravel (fluvial, | Range of particle sizes
for mortar(cement+sand), | glacial, marine), crushed | (grading), low impurities like
for asphaltic concrete or | sand and gravel, crushed | (sulphate, sulphide, organic
asphalt pavements (sand | rock, industrial waste | matter, chlorides, mica, fine
+gravel+cement or filler + | (slag) | clay materials)
bitumen), for roads (sub |  | 
base layer), for building |  | 
foundations & dams, for |  | 
water purification filters |  | 

## Slide 4
Bricks and Tiles | clay (marine, alluvial, | no excess water (plasticity
 | glacial) fired at high | index), low (iron, sulphide,
 | temperatures. | sulphate CaSO4 < 5%,
 | sand, limestone | carbonate CaCO3 < 20%),
Cement | limestone mixed with clay | constant composition (CaO,
 | converted to clinker in | Al2O3, SiO2, Fe2O3), low (S,
 | kiln, product ground to | MgO, P, alkalis)
 | powder with gypsum | 

## Slide 5
Glass | quartz or silica sand, | suitable grading grains, no
 | quartzite | impurities (low iron)
Juss, plaster, plaster | gypsum, anhydrite | no impurities (low clay and
boards |  | iron)
Insulating materials | fibrous and flaky | not injurious to health
 | metamorphic minerals | 
 | (asbestos), mica, | 
 | diatomite, vermiculite |