## Slide 1
Principal steps in the exploitation of ore
1. mineral exploration-to discover an ore body
2. Economic evaluation of the discovered ore body
3. Mine development
Mining (extraction of ore from the ground)
5. Ore dressing (mineral processing)-milling of the ore, separation of ore minerals from gangue to get ore minerals concentrates (e.g. copper concentrate).
6. smelting (recovering metals from the mineral concentrates)
7. refining (purifying the metal)
8. marketing (shipping the metal).

## Slide 2
Some important factors in the economic evaluation of ore deposit
Ore grade:
The concentration of a metal in an ore body, usually expressed as a percentage or in parts per million (ppm).
Cut-off grade:
The lowest grade of ore that can be extracted with the highest profit. The value of cut-off grade varies from one ore deposit to another and within the same metal depending on many geological and non-geological factors

## Slide 3
Factors affecting the value of cut-off grade
1- By-product
In some ores several metals are present and the sale of one may help and is enough to extract the other. For example, silver and cadmium can be by-products of the mining of lead-zinc ores and uranium is an important by-product of many South African gold ores. 40% of the gold recovered at U.S.A is by-products in the extraction of copper ore.

## Slide 4
2- Mineralogical form
The properties of a mineral affect the ease with which existing technology can extract and refine certain metals and this may affect the value of cut-off grade. Nickel is recovered far more readily from sulphide than from silicate ores, and sulphide ores can be worked down to about 0.5% whereas silicate ores must assay about 1.5% in order to be economic.
The mineralogical nature of the ore will also place limits on the maximum possible grade of the concentrate. For example, in an ore containing native copper it is theoretically possible to produce a concentrate containing 100% Cu ,but if the ore mineral was chalcopyrite (CuFeS2) ,the principal source of copper, then the best concentrate would contain only 34.5% Cu.